| Table 10.2 Comparison of Fuel Element Characteristics |  |  |
| --- | --- | --- |

|  | Thermal Reactor | Fast Reactor |
| --- | --- | --- |

| Fuel | UO2 | (U,Pu)O1.96 |
| --- | --- | --- |

| Fuel Pellet Density (% of theoretical) | 92 | 90 |
| --- | --- | --- |

| Max. fuel centerline temperature (overpower condition)°C | 2450 | 2800 |
| --- | --- | --- |

| Cladding | Zircaloy-4 | 316 Stainless Steel |
| --- | --- | --- |

| Max. cladding mid-wall temperature °C | 380 | 660 |
| --- | --- | --- |

| Coolant temperature, °C | H2O, 280-320 | Na, 470-650 |
| --- | --- | --- |

| Maximum rod linear power, W/cm | 620 | 550 |
| --- | --- | --- |

| Fuel wrapper assembly | Square, 30x30 | Hexagonal, 13 cm across flats |
| --- | --- | --- |

| # of pins in assembly | 200 | 220 |
| --- | --- | --- |

| Fuel-rod outside diameter, mm | 10.7 | 6.3 |
| --- | --- | --- |

| Cladding thickness, mm | 0.6 | 0.4 |
| --- | --- | --- |

| Initial fuel-cladding radial gap, mm | 0.08 | 0.07 |
| --- | --- | --- |

| Length of fueled portion, cm | 365 | 90 |
| --- | --- | --- |