Problem 12.4

After irradiation it was found that where the T=2000°K, the Mo was distributed as follows;

• 0.08 mole% MoO2 in oxide fuel

• 10 at% Mo in metallic inclusions

•  0.01 g of metallic inclusions per gram 					of irradiated fuel

-------------------------

a.)  Assuming ideal solutions, calculate

for Mo(s) + O2(g)<==> MoO2(s)

(eq. 12.17)

@ 2000 °K,

= - 574 + 164 •2 = -246 kJ/mole

Then oxygen potential is;

8.28• 2•ln(0.08/10)=-80 kJ/mole

= -246-80 =-326 kJ/mole

b.)  Assuming that all the noble metals are in metallic inclusions, calculate the burnup of the fuel. ( Assume all At. Wts. of elements in metallic inclusions are 100)

There are 0.01 g of metallic inclusions per g of fuel, or,

g atoms of metallic inclusions per 0.1 cm3 of fuel

----------------------------

However, only 10% (at) of inclusions are of Mo

The Noble Metal (NM) conc. (g atom/cm3 fuel) is

===============

initial heavy metal Conc

=

= 0.037 g atom HM /cc of fuel

using eq. 12.16

β= 5.3 %

c.)Find the Mo content of the metallic inclusion that should have been found if no Mo had been lost  from or gained by the unit volume of fuel under consideration.

From eq. 12.16, total Mo conc. after 5.3% BU ;

table 12.1      Part b

= 0.0004

Mo in metallic inclusions (\f(g atom,cc fuel))			= 0.001(\f(g atom incl,cc fuel)) •

assume metallic inclusion are principally NM, use b.)

Mo in fuel matrix, \f(g atom,cc fuel)

= 0.037 \f(g atom HM,cc fuel) •

But the ratio  is fixed by and is the same as the measured value, therefore,

and

= 0.0013

=

= 0.31

Metallic inclusions should have contained 31% Mo if none is lost from this spot in the fuel.  The fact that only 10 at% of the inclusion was Mo means that ≈ 2/3 of the Mo produced by fission at the radial location where the measurements were made was removed by some migration process to other radial positions in the fuel pin.