13.3.2  Xenon in UO2

Xe does not seem to migrate by;

a.)  interstitial mechanisms

b.)  simple vacancy mechanism

It is found that Xe diffuses by a combination of 1 U vacancy and 2 Oxygen vacancies.

If Xe did diffuse by vacancies;

Frac. of vacancies

on sublattice used

========================================

One could control the diffusion by controlling the vacancy concentration through chemical additions ( see Chapter 11 -12 )

========================================

With the mechanism uncertain, have to rely on empirically determined diffusion coefficients

_____________________

13.4  Reaction Rates of Atomic Size Defects

With species A and B in the matrix;

reaction rate A, B   = kAB CA CB

CA, CB  are volumetric concentrations of A, B

•  A can be mobile or stationary

•  B can be mobile or stationary

Two forms of reactions;

1.) Diffusion ( mobility ) controlled

2.)  Reaction  Rate Limited

--------------------------------------------

13.4.1  Vacancy -Vacancy Interaction

See Figure 13.4

( Dienes and Damask were the first to treat this problem )

\f(Rate of Divacancy Formation,cm3)      =   PvvCv

Pvv = 12 Px    (see fig. 13.4)

prob/s that another

vacancy jumps into

a site that is nearest

neighbor to a particular

vacancy						Px = 7 xvω

rate at which

vacancy jumps to					xv = CV Ω		a particular site

\f(#,unit vol.)            	vacancy site fraction

\f(Rate of divacancy formation,cm3) = 84 ω Ω

This gives

Remember:

This is for a fcc lattice only, it would be different for a bcc structure because would get a different combinatorial number.  If both vacancies were mobile, kvv should be multiplied by 2 .

---------------------------

13.4.2  Vacancy - Interstitial Recombination

Analogous to the divacancy case

immobile   mobile

which gives;

12    x   4

nearest        interstitial

neighbors		positions

Reason that this is not right is that interstitial atoms do not occupy nearest neighbor positions .... and ..... recombination volume is  a lot larger

Figure 13.5

get

more like

several hundred

----------------------------------------------

13.4.3   Interaction between Migrating Fission Gas Atoms

Assume that both gas atoms are mobile

do not consider reverse reaction now

Analogous to the vac - int problem

much larger than 84

-------------------------------------------

the formation of a diatomic cluster is probably a prelude to nucleation and hence is very important

rate of formation      =

of diatomic clusters

13.4.4. Interaction Between Xenon Atoms and Atomic Sized Defects

Gas atoms are not the only defects that other gas atoms can interact with, they can find point defects as well

Rate of trapping

of fission gas		=  kgtr Ct C

atoms/cm3

traps  gas atoms

as before,

-----------------------------------

\f(Rate of Gas Atom Trapping,cm3)

Trapping length

L2          =                 j                 	random 			# of jumps    lattice

walk theory		to get to 	spacing

trap