13.5 Diffusion Limited Reactions

Interaction rates have two components

1.)   Diffusion in the bulk to the defect

2.)  Reaction rate at the surface of the defect

--------------------------------------------------

13.5.1   Diffusion to Spherical Sinks

Set up unit cell - Figure 13.7

Time			Spatial	Uniform

Variation	    Variation	Production

Note :  Neglecting Recombination

at equilibrium,

Noting ;

and

C (R, t) = CR

Then;

____________________________________

Assume >> R, Figure 13.8

__________________________________

Region 1  ( neglect production rate)

and C(∞)  =  C()

Solving;

Since

Two parameters of Importance

1.) Absorption by a sphere

= - ( 4pR2) J

What is this?

2.) Absorption by all spheres

if C()  >> CR

= 4pRDCCt

rate constant

k =  4pRD

---------------------------------------------------

see page 213 for derivation of bubble radius during post Irradiation annealing

Note : only good for ideal gas

13.5.2  Diffusion to Dislocations

1.)  Switch to cylindrical co - ordinates

( p) rd  = 1

2.)  At equilibrium;

recombination

approximate this by

3.)  Exact Solution

4.)  Approximate Solution

5.)Rate of Vac. Capture by Dislocations/cm3

This is all diffusion controlled

13.5.3  Mixed Rate Control

For a reaction rate control to dislocations, the vacancy capture/cm3

= Dv Zvd rd Cv

Analogous to heat conduction, use vacancy capture/cm3 to be,(in the intermediate regime)

Reaction Rate	   Diffusion ( for rd≈1010)

≈ 0.04				≈ 0.7

Hence, the vacancy absorption is almost entirely diffusion controlled