| Physical Properties of the Six Plutonium Allotropes |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |

| Phase | Crystal Lattice | Number of Atoms Per Unit Cell | Transition to Next Higher Phase, °C | Density gm/cm3 | Coeff. of Thermal Expansion x 10-6 per °C | Volume Change on Transformation, % |
| --- | --- | --- | --- | --- | --- | --- |

| Alpha | Monoclinic | 16 | 112 | 19.8 | 46.4 | α->β, 8.9 |
| --- | --- | --- | --- | --- | --- | --- |

| Beta | Body centered Monoclinic | 34 | 185 | 17.65 | 38.4 | β-> γ, 2.4 |
| --- | --- | --- | --- | --- | --- | --- |

| Gamma | Face centered Othorhombic | 8 | 316 | 17.2 | 34.7 (a=-19.7) (b= 39.5) (c = 83.4) | γ ->δ, 6.7 |
| --- | --- | --- | --- | --- | --- | --- |

| Delta | fcc | 4 | 451 | 15.9 | -8.8 | δ->δ', -0.4 |
| --- | --- | --- | --- | --- | --- | --- |

| Delta Prime | body centered tetragonal | 2 | 480 | 16.0 | -116, (a=305) (c= -659) | δ'-> ε - 3.0 |
| --- | --- | --- | --- | --- | --- | --- |

| Epsilon | bcc | 2 | 640 | 16.51 | +36.5 |  |
| --- | --- | --- | --- | --- | --- | --- |