Terminology

• Pyroprocessing:

Pyrometallurgical and electrochemical processing

• Key Step: Electrorefining

Electrotransport in a molten salt (LiCl-KCl) electrolyte

• Electrorefining:

Metal is electronically dissolved at an anode made of impure metal and re deposited at a cathode in a condition of greater purity

Anode: M---> M+3 + 3e-

Cathode: M+3 + 3e- ---> M

Chemical Basis of Pyroprocessing

• Separations based on the relative ease 	  of oxidation into a molten salt

-Free energy of formation of metal chloride is 		primary determinant of ease of oxidation

• Some Separations are Chemically 	Complete

-Halides remain in salt as anions

-Alkali metal and alkaline earth metals (plus 		Sm and Eu) are completely oxidized and 			remain in salt

-Noble metals not oxidized; remain as metals

• Actinide and Rare Earth Metals Partition Between Salt and Metal Phases

-Can be transferred to salt by oxidation, or to metal by reduction

Pyroprocess Chemistry

• Treat as a Series of Equilibrium 	Reactions

M + M'Cl3 <---> M' + MCl3

• ΔG = Free Energy Change

•

Process is Controlled by Adjusting Redox State of Electrorefining Cell

Free Energies of Formation

| in kcal/g-mole equiv. Cl @ 500°C |  |  |
| --- | --- | --- |

| Elements that remain in salt (very stable chlorides) | Materials that can be electrotransported efficiently | Elements that remain in Cd pool as metals (less stable chlorides) |
| --- | --- | --- |

| BaCl2 87.9 CsCl 87.8 RbCl 87.0 KCl 86.7 SrCl2 84.7 LiCl 82.5 NaCl 81.2 CaCl2 80.7 LaCl3 70.2 PrCl3 69.0 CeCl3 68.6 NdCl3 67.9 YCl3 65.1 | CmCl3 64.0 PuCl3 62.4 AmCl3 62.1 NpCl3 58.1 UCl3 55.2 ZrCl2 46.6 | CdCl2 32.2 FeCl2 29.2 NbCl5 26.7 MoCl4 16.8 TcCl4 11.0 RhCl3 10.0 PdCl2 9.0 RuCl4 6.0 |
| --- | --- | --- |

Plutonium Recovery

• Chemical Reaction at Solid Cathode

-UCl3 + Pu (s) <-----> PuCl3 + U (s)

-PuCl3 is more stable than UCl3

- Deposition of Pu is favored if

(not practical)

• In the Presence of Cd, the Pu 	Chemical Activity is Greatly Lowered 	and It Behaves as though Its Chloride 	were Only Very Slightly More Stable 	Than UCl3

• Chemical Reaction-Liquid Cd Cathode

-UCl3 + Pu (Cd)  <---> PuCl3 + U (Cd)

- Deposition of Pu is favored only if

- Deposition of TRU elements occurs as the 		intermetallic compound; e.g., PuCd6

- U also deposits in a quantity roughly equal  		to the TRU elements